## Slide 1: Copper surface: Oxide Removal in Acid
CuO + 2H3O+ → Cu+2 + 3H2O
Depending on the history of the Cu surface, there may be other types of oxide on the Cu surface, e.g., Cu2O, CuOH and Cu(OH)2, for which similar reactions may be written.

## Slide 2: Pd Catalyzation of Cu Surface
Cu0 → Cu+2 + 2e- … localized reaction
Pd+2 + 2e- → Pd0 … localized reaction
------------------------
Cu0 + Pd+2 = Cu+2 + Pd0 … Overall reaction
Both of the above “half” reactions may occur on slightly-separated, nanoscopically-different regions of the Cu surface.

## Slide 3: Electroless Ni(P) Reactions
H2PO2- → H2PO2-(ads) … Initially occurs on Pd catalyst surface
H2PO2-(ads) → HPO2-(ads) + H0(ads)
HPO2-(ads) + OH- → HP(OH)O2- + e- … provides electron for Ni+2 reduction (unverified reaction)
There may be different reactions involving hypophosphite oxidation (will figure out in next few weeks)
Ni+2 + 2e- → Ni0 … nickel deposition reaction
H2PO2-(ads) + 2H3O+ + e- → P + + 4H2O … phosphorus co-deposition
H0(ads) + H0(ads) → H2 … hydrogen gas evolution reaction
The above “half” reactions may occur on slightly-separated, nanoscopically-different regions of the Cu surface.