## Slide 1
To make 1.5L of 0.1g PdSO4 per liter of 5% H2SO4 stock:
Add 0.15g PdSO4 (analytical reagent grade) to 1.5L of 5% H2SO4 acid mixture (see preparation procedure)
*Note: PdSO4 takes time to dissolve; allow at least two days of overnight stirring (if solution level gets low, add more 5% H2SO4 to mark before transfer)
The seed solution is filtered (see Figure 1) prior to use.
*Note: for FRESH solutions, use 0.2um filter initially then follow with 0.05um filter
for USED solutions, only filter with 0.05um

## Slide 2
CATCH BASIN
Figure 1. PdSO4 Reagent Filtration Set-up