## Slide 1
10.5 L Ni(P) bath
fresh
2.5 L Ni(P) bath
for replenishment
after every 30++ wafer runs
Take-out OLD 2.5L mixture, measure pH
Add NEW 2.5L Ni(P) mixture:
1,913 mL H2O
500 mL ANP-M
85 mL ANP-N
2.5 mL Brightener
Filter, measure pH (~4.3 – 4.2) AND using 5% H2SO4, bring pH down to about 3.98
8.0325L H2O, 2.1 L ANP-M, 0.357L ANP-N, 10.5mL Brightener pH ~4.85
use 5% H2SO4 to bring down to pH 3.98, note final pH

## Slide 2
1 L Ni(P) bath
fresh
765 mL H2O, 200 mL ANP-M, 34 mL ANP-N, 1mL Brightener pH ~4.85
use 5% H2SO4 to bring down to pH 3.98, note final pH