## Slide 1
NiPU30
10/30/2019
Fresh 10.5 L bath (2nd time fresh 10.5-L bath was made)
SEM cross-section result:
48nm for 50 sec (0.83min)
 57.8 nm/min
Copper Dummy Profilometer scans:
Profilometer_Step-height
measurement result:
AVE: 785nm for 10min
 78.5 nm/min
START of
RUN
END of
RUN
NS_JT5A monitor for SEM:
Decided on:
55s Plating Time
 53 nm NiP thickness
(based on SEM)